## Slide 1
Design of a FRP running blade
Gabriele Decortes
Fabio Marchi
Emanuele Nicolò Pizzo

## Slide 2
FRP
Stacking sequence
Weight
Running blade
Short distance running
Long and high jumping
Project overview

## Slide 3
History of lower limb prostheses
Egyptians and Romans
Wars and conflicts
Renaissance
Terry Fox and Van Phillips
SACH foot
Today

## Slide 4
Liner
Avoids friction and movements
Silicon or polyurethane
Socket
Allows control of the prosthesis
Rigid or flexible
Blade
Acts as a spring to transmit energy
C-shaped or J-shaped
Composition of RSPs

## Slide 5
Spring-mass system
Composition of RSPs
Energy efficiency < 240%
Energy efficiency < 90%

## Slide 6
Manufacturing technology
Preliminary work
2D laminates
3D woven
Classical methods
Hand lay-up
Prepreg Vacuum-Bagging
Resin transfer moulding
Innovative methods
Prior incorporation
Incorporation in the nozzle
Incorporation on the component

## Slide 7
Static analysis

## Slide 8
Model construction (1)

## Slide 9
Model construction (2)
Material: lamina
Mesh: 2140 elements (S4R)
BCs: encastre
Load type: pressure

## Slide 10
Composite layups; starting laminates
[0, 45, -45, 90, 0, 0, 90, -45, 45, 0]s
[0, 45, -45, 45, 0, 0, 45, -45, 45, 0]s

## Slide 11
Composite layups: optimization pattern
[0, 45, -45, 90, *, 0, 0, 90, -45, 45, *, 0]s
[0, 45, -45, 45, *, 0, 0, 45, -45, 45, * 0]s
[45, 90]n packets at *
[±45]n packets at *
Tsai-Hill < 1
δ= 4 cm

## Slide 12
Materials
CFRP
E1 = 177 GPa
GFRP
E1 = 43 GPa
Aluminium
E = 72 GPa
ρ = 1.6
ρ = 1.6 〖𝑔/𝑐𝑚〗^3
ρ = 2
ρ = 2 〖𝑔/𝑐𝑚〗^3
ρ = 2.8
ρ = 2.8 〖𝑔/𝑐𝑚〗^3
E2 = 10.8 GPa
E2 = 8.9 GPa
𝜈 = 0.33
𝜈12 = 0.27
𝜈12 = 0.27
G12 = 7.6 GPa
G12 = 4.5 GPa
CFRP
GFRP
Aluminium

## Slide 13
Results

## Slide 14
Results
Objectives
Maximum displacement = 4 cm
Lowest possible weight
Stacking sequence

## Slide 15
Results
Objectives
Maximum displacement = 4 cm
Lowest possible weight
Stacking sequence

## Slide 16
Results
Objectives
Maximum displacement = 4 cm
Lowest possible weight
Stacking sequence
  CFRP
GFRP
52 plies
13 mm thickness
1.75 Kg
82 plies
20.5 mm thickness
3.5 Kg

## Slide 17
Results
Objectives
Maximum displacement = 4 cm
Lowest possible weight
Stacking sequence
Aluminum
12 mm thickness
2.8 Kg

## Slide 18
Results
Objectives
Maximum displacement = 4 cm
Lowest possible weight
Stacking sequence

## Slide 19
Manufacturing
Fast process with high quality capability but the investment cost does not justify its use for running blades
Cheap and simple process but subject to high variability and lower quality
Cheaper process with respect to RTM, still guranteeing high quality at lower costs
Hand lay-up
RTM
Prepreg Vacuum Bagging

## Slide 20
Cost evaluation: contributions
Raw materials
Post processing
Prepreg vacuum bagging
Personalization through optimization
Low production numbers
Metallic inserts
Certifications and brand name
  No reference on the market for processes and brands

## Slide 21
Cost evaluation: results
≅ 15000 €
Raw materials
R&D
Manufacturing
Mark-up
3-5x

## Slide 22
Conclusions
Geometry
Composite properties
Loads and BCs
Layup optimization
Materials choice

## Slide 23
Thank you for your attention